ENMA410 - Materials for Energy 1

Spring 2020

Lecture: 	Tuesdays and Thursdays, 12:30 pm - 1:45 pm

MTH 0403

Office Hours: 	By appointment - please email to schedule

Professor: 	Eric D. Wachsman

ewach@umd.edu

Room 1206, Bldg. 089

Teaching Assistant: 	TBD

Credits:	3

Recommended Texts:

Fundamentals of Materials for Energy and Environmental Sustainability

Edited by David Ginley and David Cahen, Cambridge University Press

Advanced Batteries, Materials Science Aspects

Robert A Huggins, Springer

Fuel Cell Fundamentals

Ryan O’Hare, Suk-Won Cha, Whitney Colella, and Fritz Prinz, Wiley

Additional reading and lecture materials will be distributed

## Grading:	Homework - 20%

2 Mid Term Exams - 20% each

Final Exam - 40%

## Course Description:

## The goal of Materials for Energy is to demonstrate the role of materials in solving one of the most critical socio-economic issues of our time, affordable and sustainable energy.  Materials for Energy is a two-part course based on material functionality, however, they are independent and neither is a prerequisite for the other.

## Materials for Energy 1 will start with a discussion of U.S. and global energy and related environmental issues.  It will then focus on electrochemical, chemical, and nuclear functional materials.  Topics to be covered include: fuel cells and batteries (electrochemical energy conversion and storage); catalysts and membrane separations (fossil fuel and biomass energy conversion); and nuclear fuels.

## Course Outline

## Topics:                    	Tentative Dates:

- Introduction to Energy:	Jan 28

  - Resources

  - Efficiency and demand

- Environmental impacts: 	Jan 30

  - Climate change and air pollution

  - The energy-water nexus

- Electrochemical energy storage: 	Feb 4-25

  - Introduction to batteries and capacitors

  - Ionic transport

  - Electrolytes

  - Anodes

  - Cathodes

* Guest Lecture, Dr. Kang Xu, Army Research Lab	Feb 6

- Midterm exam: 	Feb 27

- Electrochemical energy conversion: 	March 3-26

  - Introduction to fuel cells

  - SOFC electrolytes

  - SOFC anodes and cathodes

  - SOFC interconnects and seals

  - PEMFC electrolytes

  - PEMFC anodes and cathodes

* Guest Lectures, Dr. Yi-Lin Huang, Maryland Energy Innovation Institute

* Spring Break 	March 17, 19

- Membrane separations: 	March 31-April 7

  - Introduction to membranes

  - Porous membranes

  - Dense membranes

- Midterm exam: 	April 9

- Engineering Sustainability -50th Earth Day Anniversary	April 21

- Catalytic conversion: 	April 23-May 5

  - Introduction to catalysis

  - Oxide catalysts

  - Nobel metal catalysts

  - Membrane reactors

- Nuclear fuels:	May 7

- Course review:	May 7

Electrochemical Society Meeting	May 12, 14

Final Exam (1:30 pm – 3:30 pm):	May 19