ENMA 471

Kinetics, Diffusion and Phase Transformations

Instructor: 	Prof. Ray Phaneuf

CHE1108

(301) 405-6566

phaneuf@umd.edu

Office Hours: Tuesdays, Thursdays 12:30-13:30, or by appointment

Teaching Assistant:  Weiran Zhang

CHE2132

weiranz@umd.edu

Office Hours: TBA

Class Meets:	Tuesdays, Thursdays from 11:00-12:15

IRB 0324, Zoom

Course Description: Fundamentals of diffusion, kinetics of reaction including nucleation, growth and phase transformations are discussed.  Topics include diffusion in substitutional solid solutions, interstitial diffusion, nucleation and growth theories, solidification, diffusional transformations and growth of crystalline solids.

Prerequisites: ENMA 461

Textbook: “Phase Transformations in Metals and Alloys”, D. A. Porter and K. E. Easterling, 2nd ed. (New York, Chapman & Hall, 1992) (required).

“Crystal Growth for Beginners”, I.V. Markov (World Scientific, Singapore, 2003) (suggested).

Other Useful References:

“Thermodynamics and Kinetics in Materials Science, a Short Course”, B. S. Bokstein, et al. (Oxford, UK 2005); “Diffusion in Solids”, 2nd ed., Paul Shewmon (Minerals, Metals, & Materials Society, 1989); “Lectures on the Theory of  Phase Transitions”, ed. H. Aaronson, (American Institute of Mining, Mineralogical and Petroleum Engineers, New York, 1975);  “Fractal Concepts in Surface Growth”, A. L. Barabasi and H. E. Stanley, (Cambridge University Press, 1995); “Physics of Crystal Growth”, A. Pimpinelli and J. Villain (Cambridge University Press, 1998).

Website: Class materials and assignments will be posted at https://myelms.umd.edu/

.

Course Objectives: A student who takes this course should learn:

(1) about thermal activation and the relationship to kinetics

(2) to solve diffusion problems, both steady state and transient,

(3) about coarsening and grain growth and

(4) about the role of interfaces on transformations.

Topics Covered:

Topics						References

Review of Thermodynamics	Porter & Easterling Ch. 1 & Supplements from Technical Literature

Equilibrium

Single Component Systems

Binary Solutions

Equilibrium in Hetrogeneous Solutions

Diffusion	Porter & Easterling Ch. 2 & Supplements from Technical Literature

Atomic Mechanisms

Interstitial Diffusion

Substitutional Diffusion

Atomic Mobility

Tracer Diffusion in Binary Alloys

Diffusion in Ternary Alloys

High Diffusivity Paths

Diffusion in Multiphase Binary Solutions

Crystal Interfaces and Microstructures	Porter & Easterling Ch. 3 & Supplements from Technical Literature

Interfacial Free Energy

Solid Vapor Interfaces

Boundaries in Single Phase Solids

Interphase Boundaries

Interface Migration

Solidification	Porter & Easterling Ch. 4 & Supplements from Technical Literature

Nucleation

Growth of a Pure Solid

Alloy Solidification

Diffusional Transformations in Solids	Porter & Easterling Ch. 5 & Supplements from Technical Literature

Homogeneous Nucleation

Heterogeneous Nucleation

Precipitate Growth

Transformation Kinetics

Spinodal Decomposition

Ordering Transformations

Diffusionless Transformations	Porter & Easterling Ch. 6

Shape Memory Effect

Additional Topics (As Time Permits)

Thin Film Growth	Markov Ch. 2 & 3  & Supplements from Technical Literature

Diffusion in Polymers and Reptation

Grading:

Homework 						30%

Midterm Exam					30%

Final Exam						40%

Relationship of course to program objectives: This course is one of the senior-level required courses in Materials Science and Engineering at the University of Maryland, and is intended to contribute toward the program objectives of (1) producing high quality  graduates, (2) making sure that students can define and solve engineering and science  problems, and (3) providing fundamental knowledge of materials to allow graduates to function professionally as materials scientists and engineers.

Assignments, Classroom Etiquette and Academic Ethics: Homework and outside reading is essential to master the material covered in this class.  Readings should be done in advance to allow discussion during the class periods.  Homework is generally due at the beginning of class one week after being assigned.

Attendance is suggested, but not required, outside of exams and when in-class presentations are scheduled.  Classroom etiquette includes switching off cellular phones and leaving reading of unrelated material (newspapers, etc…) to outside of class.

Working together on homework assignments is strongly encouraged, but copying answers from previous years is not allowed, and considered to be cheating.  Cheating and plagiarism on homework, exams and presentations are violations of the University Code of Academic Ethics, and will not be tolerated.  Please see http://www.shc.umd.edu/code.html for a detailed discussion of this important issue.